| NTC Thermistors |  |
| --- | --- |

Category Type Style Resistance Range (Ohm) Reference Temp. () Resistance Tolerance (%) B Constant B Constant Tolerance (%) Temp. Range () PDF NTC thermistors NT73 SMD 1k 150k 25 5, 10, 15 3200K 4100K 3, 5, 10 −55 +125

|  | PTC Thermistors |  |
| --- | --- | --- |

Category Type Style Resistance Range (Ohm) Reference Temp. () Resistance Tolerance (%) CurieTemp. Temp. Range () PDF PTC thermistors PT72 SMD 50 1k 25 50 70,80,100 −55 +125

|  | Linear P.T.C. Resistors/Thick film |  |
| --- | --- | --- |

Category Type Style Resistance Range (Ohm) Reference Temp. () Resistance Tolerance (%) T.C.R. Temp. Range () PDF Linear P.T.C. resistors/Thick film LA73 SMD 22 10k 25 5 1000 3600 (×10−6/K) −55 +125

|  | Linear P.T.C. Resistors/Thin film |  |
| --- | --- | --- |

Category Type Style Resistance Range (Ohm) Reference Temp. () Resistance Tolerance (%) T.C.R. Temp. Range () PDF Linear P.T.C. resistorsThin film LT73 SMD 51 51k 25 2, 5 150 4500 (×10−6/K) −40 +125 LT73V SMD 51 22k 25 2, 5 150 4500 (×10−6/K) −55 +155 LP73 SMD 100 10k 25 1, 2, 5 3000 5000 (×10−6/K) −55 +125 MLT MELF 1k 9.1k 25 5 2000 3900 (×10−6/K) −40 +125 LT Leaded 100 39k 25 5 1000 4500 (×10−6/K) −40 +125 LP Leaded 1 100k 25 1, 2, 5 150 5000 (×10−6/K) −55 +150

|  | Platinum Thin Film Thermal Sensors |  |
| --- | --- | --- |

Category Type Style Resistance range (Ohm) Reference temp. () Resistance tolerance (%) T.C.R. Temp. Range () PDF Platinum thin film thermal sensors SDT73H SMD 100, 500 0 0.2, 1 3850 (×10−6/K) −55 +155 SDT73V −55 +155 SDT101A Leaded 10, 100, 500 0, 25 0.5, 1 3500 (×10−6/K) −55 +150 SDT101B −55 +300 SDT310LTC Leaded 100, 500, 1k 0 0.059 0.12, 0.39 3850 (×10−6/K) −55 +155 SDT310P −55 +400 SDT310MTM 100 0.12, 0.39 −55 +650 SDT310HLTC 1k 0.059 0.12, 0.39 −55 +155 SDT310AP 10 10 −55 +400 ST Special form (custom) — — — — — AFS — — — — —

Common Specification (Thermal Sensors) Items PDF Minimum Ordered Quantity Recommended Pad Dimensions Packagings For Chip Components Axial Tapings Color code•Resistance marking•E series numbers