Heading filter is the market leader in dust to air filtration, working with companies around the world to endure that their only output into the workplace and local environment is clean air. Wherever dust is created, Heading filter bags can provide the solution. Having been in the business for over 20 years. we make certain that you get the right bag filter for your application by considering all appropriate aspects of your decision. In addition, we offer a complete line of replacement and custom designed bag filters to fit all manufacturer filter bag housings.

All of our filter bags are available in many different weights, treatments and coatings to suit the industry application.

Standard and specific media materials are

Fabrics

Polypropylene

Polyester

Acrylic

Nylon

Teflon

P84

Nomex

Ryton

PTFE

Wool

Cotton

Glass

Ceramic

Available Coating and treatment

Acrylic coating

Antistatic treatment with carbon fiber

Antistatic treatment with copper wire

Antistatic treatment with stainless steel fiber

Water and oil repellent

PTFE impregnation

PTFE coating

Media with PTFE laminated

Areas of application

Cement and lime industries

Steel and aluminum industries

Steel and aluminum industries

Incineration Plants

Coal-Powered Plants

Toxic fumes filtration in the ceramics industry

Gas filtration at high temperatures

Services

Analysis and testing laboratory

Consultancy service

Monitoring of filtration media

Supervision and installation of bags

Liquid filter bag

Heading filter is a leading supplier of filter bags, filter cartridges, filter housing, and media filters designed to meet the requirements of all types of liquid filtration applications.

Styles of filter bag media

FELT

Available in polyester and polypropylene , felt is generally used when particle retention of 1-200 microns is required . Felt media provides three dimensional depth filtration , resulting in a much higher solids loading capacity over the equivalent area of mesh fabric.

Mesh

Nylon monofilament – A woven fabric with evenly spaced holes. Suitable for surface filtration only, monofilament consists of single untwisted, bags are available in 25-800 microns.

Polyester multifilament

Also suitable for surface filtration, this low cost, disposable fabric consists of many smaller smaller diameter threads twisted together . Available in 100-800 microns.

Convention Chart

Mesh  12000   5000  2500  1250  625  550  300  200  140  120  100

μm    1       3     5     10    20   25   50   70   100  125  149

Mesh  70       60    50     45   35   30    25   20   18   16    14

μm  200      250   300   350   500  590   710  840  1000 1200  1400

Material physical and chemical performance

Material       PE        PP         MO        RY          PTFE

Strong Acid   very good   excellent     poor       general       excellent

Weak  acid   very good   excellent     general     good         excellent

Strong Alkalis  very good   excellent    excellent    very good 	 excellent

Weak Alkalis   very good   eceellent    excellent     good         excellent

Solvents       very good   poor        good        good        very good

Oxidizing Agent good       poor        general       good        good

Abrasion Resistance very good  very good  excellent     general       poor

Application

Heading Filter Material Co., Ltd  manages the production of liquid filter bags from fiber processing to the manufacturing of finished filter bags.

We offers custom- sized and custom- shapes bags in a variety of materials.

Material and micron rating

Polypropylene felt    Micron rating available in 1,3,5,10,25,50,100.

Polyester felt     Micron rating available in 1.5.10.25.50.75.100.200.

Nylon Mesh  Micron rating available in most sixes

Polypropylene  Mesh  Micron rating available in most sizes

High Temperature Teflon Mesh   Micron rating available in most sizes

High Temperature Micron Rating Nomex Felts available.

Sizes                           Styles

#1-----(7"x16")                   Plastic Ring

#2-----(7" x 32")                  Metal Ring

#3-----(4"x 8 1/4")                 Draw string

#4-----(4"x 14")                   Plain

Available Materials

Nylon Monofilament

Polyester Multifilament

Polypropylene Monofilament

Polyester Monofilament (requires special order)

Standard filter bag

Standard filter bag includes a steel ring collar that is designed to gasket as well as support and secure the filter bag when placed into the bag housing.

Nylon mesh(monofilament) liquid filter bag

Steel ring stitched filter bag

Plastic welded liquid filter bag

Welded bag was designed to meet the following requirements

NO needle holes

No thread contamination

Precision bonded cutting of the fabric edges

Maintain same efficiency as filter media

Plastic collar filter bag

Plastic collar was engineered to meet the following requirments

Molded plastic with built-in handle makes installation and disposal faster, cleaner, and less expensive.

100%  incinerating ability

Just drop into  housing and push down

Smooth plastic designs prevent build-up of contaminants around header

Collar is sewn into place to ensure that plastic and media remain  firmly intact throughout filter life.

Oil adsorption bags

Material and micron rating

Polypropylene felt Micron rating available in 1, 3, 5, 10, 25, 50, 100

Polyester felt micron rating available in 1, 5, 10, 25, 50, 75, 100, 200

Styles   Plastic ring , Metal ring

Micron rating filter bag specifications

Bag size  Flow area  Volume   Diameter   Length      Max Flow

(m2)       (L)     (inch/mm)   (inch/mm)   (m3/hr)

HT-1     0.19        7.9     7/178       16/450      20

HT-2      0.41       1703    7/178       32/810      40

HT-3      0.06        1.4     4/102       8.25/230     6

HT-4      0.09        2.5     4/102       14/380       12

Heading filter

Heading filter is an industry leader in developing custom filtration fabric for many different applications

Experienced filtration fabric weaving and construction

Whether your filtration process includes waster water treatment, water supply, food processing, pharmaceutical processing. Chemical processing, or pigment and coating processes. Warwick has the technology and experience needle to fulfill your filtration fabric needs. We have broad experience in procession synthetic fibers. We can match fiber types and yarn polymers best suited to your filtration requirements, including olefin, fluorocarbon, aramid , polyethylene, nylon, and polyeater, among others.

Features

Anti Acid and weak Alkali

Oxygenation resistant

High tensile strength

Moisture resistant

Wearable

Easy to wash

Specifications

Manufacturing filter press pc. From woven and nonwoven filter media.

Filter press pcs. For wooden filter press, cast iron filter press, PP filter press, Recess filter press, membrane filter press etc.

For plate size(square)

18 "x20", 24"x24", 30"x30", 32"x32", 36"x36", 40"x40", 48"x48", 60"x60" inches.

For, Plate size (Round

18"Dia, 24" Dia, 30" Dia, 32"Dia, 36"Dia.

Applications

Standard filter presses

Membrane filter presses

Cartridge filter, electrophoresis, reverse osmosis, belt presses , vacuum belt filters, gravity belt filter, candle filters, and bag filters.

Our filter experience supports application for water and food , as well as medical product filter applications for liquid , gases and membranes.

We provide filtration cloth for various types of vacuum filters. Such as drum type filter, belt type filter, disc type filter and horizontal belt filter.

Press filter

Amongst various types of press filter for liquid / solid separation , there filter clothes are available in different sizes and colors to cater the needs of the customer.

Horizontal belt filter

Amongst various types of vacuum filter for liquid /solid separation, there is great demand for the horizontal belt filter.

Centrifuge

We provide strong and thick filtration cloth for use in centrifuge applications.

Our G-series is most suitable for fine particles filtration.

Vacuum filter

We can draw on a database containing  alithe  technical properties---- drawings , merchandise data and basic specifications handled by CAD systems in the projects department.